## Slide 1: ECE 260C, Spring 2025 On Manufacturability
Andrew B. Kahng
Kahng ECE 260C SP25

## Slide 2: “PPAC” = ?
PPAC is why the industry continues “Moore’s Law scaling”
  Must see sufficient benefit from move to the next technology node
Power, Performance, Area
  Dynamic/Static power, SAIF/VCD, …
  Incremental STA-driven sizing + buffering + synthesis operations
  Better floorplans, better P&R tools, better “Opt” (remove overdesign)
What about Cost?
  Yield = fraction of chips produced that are “good” (sellable)
  Cost of chip: (cost of fabricating, testing a wafer) / (yield * #chips/wafer)
    Higher yield is good (Manufacturability); higher #chips/wafer also good (Area)
  “good” means passing both functional and parametric criteria
    Functional: works correctly
    Parametric: is sellable (performs at spec, not too leaky, won’t fail in a week, …)
Kahng ECE 260C SP25

## Slide 3: Functional Yield
No physical faults: “opens”, “shorts” etc.
  DFT, ATPG, ATE, … spans EDA and Test supplier industries
“Critical area” = vulnerability to particular defect sizes see the dashed outlines
How much of my layout will suffer an “open” if an open spot of a particular size were to randomly appear?
  Wider wires  layout is less vulnerable
How much of my layout area will suffer a “short” if extra material of a particular size were to randomly appear?
  Wider spaces  layout is less vulnerable
Kahng ECE 260C SP25
“Spread, Fatten and Fill”
Notes: Critical area – vulnerability to particular defect sizes (see diagram)
  The area is the point of center of circular failure spots (open/short) given a specific size of spot
  Open fault areas are centered on wire
  Closed fault areas are centered on spacing between two wires
  → wider wires = fewer opens, wider spacing = fewer shorts
  “Spread (out wires), fatten (wires to make wider), and fill (free area)” methodology in early 2000s to improve manufacturability
Cost of failure goes up by 10x at every stage – problem caught at design time vs manufacturing vs packaging vs shipping vs …

## Slide 4: Enormous Engineering Efforts …
Modeling of defects
  E.g., clustering
Cleanroom technologies
  E.g., factory layout, airflow, robots, …
  “Class 1 cleanroom” etc. link
“Design for Manufacturability”
  E.g., to first order, make chip smaller (~cubic yield loss w/area)
  Better layouts: “Spread, fatten, fill”, avoid risky patterns, follow “recommended rules” aka “DFM rules”, …
  Redundancy / error tolerance
    Doubled vias and contacts
    Error detection/correction in memories
  Better OPC / mask flows
  DFM  DTCO (design-technology co-optimization)  STCO link link link
Kahng ECE 260C SP25
Note: hard to cleanly separate timing, power, reliability, yield …

## Slide 5: NDR, Redundancy Levers

## Slide 6: Specification of NDRs in LEF, DEF
…
NONDEFAULTRULE NDR3W3S
LAYER M1
WIDTH 0.07 ;
SPACING 0.07 ;
END M1
LAYER M2
WIDTH 0.21 ;
SPACING 0.21 ;
END M2
LAYER M3
WIDTH 0.21 ;
SPACING 0.21 ;
END M3
….
END NDR3W3S
END LIBRARY
NDR name
Single-width and –spacing (default rule)
Triple-width and -spacing
UNITS DISTANCE MICRONS 2000
…
NONDEFAULTRULE NDR3W3S
- net1
+ LAYER M1 WIDTH 140
SPACING 140
+ LAYER M2 WIDTH 420
SPACING 420
+ LAYER M3 WIDTH 420
SPACING 420
….
….
END NONDEFAULTRULES
…
END DESIGN
LEF
DEF
Notes: Note the difference in LEF (defined in microns) and DEF (defined in DBU, 2000 DBU = 1 micron)

## Slide 7: Track Impact of NDRs
Track cost = Number of routing tracks unavailable to the detailed router because of increase in the required spacing to neighboring wires when applying NDRs
Key: Router centers each wire segment on a track gridline
(a) 1W1S, track cost = 1
(b) 2W2S, track cost = 3
(c) 4W4S, track cost = 7
5
4
3
2
1
track #
3
2
1
1W
1S
6
5
4
3
2
wire segment
Routable Region
4W
4S
7
1
Routable track
2S
2W
Occupied track
8
9

## Slide 8: Use of NDRs in Clock Routing
Eliminate noise
  Coupling capacitance induces delay uncertainty  increase spacing
Prevent EM violation
  Large buffers driving minimum-width wires violate current density limit  wider wires have improved EM/IR robustness
Reduce variation
  Smaller geometries and more resistive interconnects (and, multiple patterning steps) induce large variations of parasitics and delays  wider wires have less variation
Reduce power (complementary: reduce skew)
  Wide wires have larger capacitance and increase dynamic power  motivates “Smart NDRs” (e.g., by wire tapering) to reduce capacitance
Kahng ECE 260C SP25

## Slide 9: Smart NDRs for Clock Power Reduction link link
Vicious vs. Virtuous cycles: Fixed NDRs vs. Smart NDRs
Can optimize wire segment widths in a clock subnet
Notes: Smart NDRs
  Smaller capacitance → fewer/smaller clock buffers/power usage
  Uses tapering – selecting smaller wire segment width in a clock subnet
  Avoids viscous cycle (pictured)

## Slide 10: Via Doubling For Redundancy
Single-cut via 
Double-cut via (“via doubling”)
  During Routing?
  or After Routing?
Why redundant vias?
  Improve yield: redundant via is “insurance” for via opens
  Improve timing yield: the resistance of partially blocked vias increases
  Reservoirs of metal for electromigration reliability
  Etc.
Observation:
  The first 70-80% of vias can be easily doubled even for very congested designs
Notes: Redundant Vias is a technology for yield improvement, which doubles single-cut via.
Via doubling can be performed during routing or after routing.
Via doubling is recommended by manufacture since it can improve yield, i.e., redundant via is “insurance” for via opens.
It can also improve timing yield since the resistance of partially blocked vias increases which may affect timing yield.
One observation is that 70-80% vias can be easily doubled even for very congested designs.
The question is: can we improve more?

## Slide 11: Short-Loop Paths to Add Redundancy
Short-loop paths
  Create detours to double vias which cannot otherwise be doubled with an adjacent single via (figure: via “v” is made redundant with a short loop)
  Up to 97.5% via doubling coverage by IBM Boeblingen in early 2000’s
    May lead to antenna / timing issues
Kahng ECE 260C SP25
Notes: We may use short loop paths to create detours to double the vias which can not be doubled with single via.
Up to 97.5% via doubling coverage is reported in ISQED 2006 paper.
However, short loop paths may lead to antenna problems and timing issues since it introduce more redundant wires.
So, can we have 100% via doubling coverage with short loop paths?

## Slide 12: CMP Fill
https://vlsicad.ucsd.edu/Publications/Journals/j40.pdf
https://vlsicad.ucsd.edu/Publications/Journals/j84.pdf
Notes: CMP (Chemical-Mechanical Planarization/Polishing)
  The top of the wafer is polished off with slurry – used to size metal/oxide layers, make chip thinner, and maintain thickness required to reduce lithographic “defocus”

## Slide 13: Planarization = Flat Wafer Topography
Planarize oxide
  Starting topography depends on layout pattern
  Figure: D. Ouma, MIT 1998
Planarize copper
  Multiple materials
  Erosion of dielectric, dishing of wide (soft) metal  “slotting” needed
  Figures: T. Tugbawa, MIT 2002

## Slide 14: Manufacturability: Layout Density Control (“Fill”)
Area fill or “dummy fill”: electrically inactive; floating or grounded
Area fill insertion (and, slotting)
  Decreases local density variation ( area density design rules)
  Decreases post-CMP interlayer dielectric (ILD) erosion, conductor dishing
    CMP: Chemical-Mechanical Polishing (Planarization)
  Cf. “Filling and Slotting: Analysis and Algorithms”, ISPD-98
Post-CMP ILD thickness
Features
Area fill
features
Must satisfy min, max area density limits in all windows of given size and “step” (e.g., density between 20-80% in 100um x 100um windows, with step size = 25um)
Notes: Area insertion must meet (crude) ruleset from foundry.

## Slide 15: Other Examples https://vlsicad.ucsd.edu/Publications/Journals/j84.pdf
Top (l-r): traditional, staggered, alternating, basket-weave why?
Bottom: diamond and plus-sign patterns
Notes: Two common modes of dummy fill – tiled/staggered vs. Track-like dummy fill
  Tiled reduces capacitances, Larger tiles reduce data sizes for GDS.
Other fill patterns existed (pictured above)
  In the 90’s, fill designs were considered highly proprietary to different design houses, with different designs primarily aiming to reduce parasitic coupling

## Slide 16: OpenROAD: “max”, “fixed pattern” (types)
https://openroad.readthedocs.io/en/latest/main/src/fin/README.html#example-scripts
“fin” = layout finishing
Metal fill can be part of output gds (foundry can insert fill as well)
SKY130 M5 example: fixed pattern = fixed density of 42.5% (how did I see this?)
Notes: fin is the layout finishing module in OpenROAD that can insert fills (the foundry can also insert fills after receiving the GDS)
  Support for OPC-like fill (thin wires running next to existing wires) and non-OPC fill (rectangular tiles)

## Slide 17: “Smart Fill” https://vlsicad.ucsd.edu/Publications/Journals/j40.pdf
Note: many ways that “dummy fill” can be smarter
  Less data volume (GDS, OASIS compressibility)? Friendly to IP reuse? Smooth density gradient? Grounded fill for PI/SI? Timing-aware,-fixing? Control both area and perimeter of metal layout? (see papers at https://vlsicad.ucsd.edu)
One key type of “smarter”: don’t add a maximum amount of fill !!!
  Capacitance = delay and power; data volume considerations as well
“Optimal” fill: minimize “M” in the linear program https://vlsicad.ucsd.edu/courses/cse101-w18/slides-w18/cse101-w18-Lecture13-linearprog.pdf
“Fill slack” = maximum amount of fill that can possibly be added into a given “file”

## Slide 18: OpenRCX
Thanks: Dimitris Fotakis and David Overhauser

## Slide 19: Capacitance Extraction
What is distribution of charge on conductor surfaces and in dielectrics?
  Solve Maxwell’s equations  electric field and potential everywhere
C = Q/V  obtain capacitance values
Slow and accurate: 3D field solvers
Quick and dirty: 1D (per-unit length total cap) or 2D (per-unit area cap + per-unit length lateral, fringing cap)
Good in practice: 2.5D  2D + corrections for adjacent layers
OpenRCX is a 2.5D method
Key challenge: building the (lookup table, interpolation) model for “corrections …”

## Slide 20: DAC 1997: “Five Foundations”
https://vlsicad.ucsd.edu/Publications/Conferences/69/c69.pdf
Foundations (1997) for lookup tables and interpolations
  1. Shielding effects of ground, and same-layer neighbors
  2. High metal density on Layer i (e.g., with dummy fill !) decouples Layers i-1, i+1
  3. Layers i  2 can be treated as ground planes; no need to look beyond
  4. Left/right same-layer couplings can be treated independently, and neighbor widths have little impact
  5. Above/below crossunders can be treated independently
Systematic design of experiments (patterns), use of field solvers

## Slide 21: Can Go Much Deeper (e.g., Fill Impact)
https://vlsicad.ucsd.edu/Publications/Conferences/205/c205.pdf

## Slide 22: OpenRCX in the Design Flow
Floorplanning
Placement
CTS
Routing
OpenRCX
STA
Floorplanning
Placement
CTS
Routing
OpenRCX
STA
Metal Fill Gen
Model File (1)
No Metal Fill Flow
Metal Fill Flow
Model File (1) - No Metal Fill including in Pattern Modeling
Note 1: if metal fill is present in the design it will be extracted as grounded wires.
Note 2: The challenge is that metal fill consideration is much larger area than pattern size; existence of fill must be either explicit or built in the extractor
Thanks: Dimitris Fotakis and David Overhauser

## Slide 23: OpenRCX Internal Flow
Read Design (LEF, DEF, ODB)
Net Connectivity
Read Model File
RC Graph Generation
Build Geometry Structures
Extract Resistance per Wire
Extract Capacitance per Wire
Thanks: Dimitris Fotakis and David Overhauser

## Slide 24: Extraction Model Creation

## Slide 25: (2.5D) Extraction Model Creation
Determine the characteristics of the process from the foundry technology information (e.g. itf or ict file)
  Layer specs, wire shape, dielectrics stack, WEE tables, Thickness tables, Rho tables, …
Create a large number of patterns of interconnect and transistor-level test structures
  Interconnect-level test structures differ from transistor-level structures
Run each pattern through a golden reference extractor
  Field solver requires proper shape, enlargements, thickness and dielectrics
Based on golden reference results, build extraction models
Verify model results versus test results and design layouts
Thanks: Dimitris Fotakis and David Overhauser

## Slide 26: Golden Reference Tool to Build Models
Process
Tech
File
Golden
Data
Test
Patterns
(drawn)
Test Patterns
(physical)
Pattern
Generator
Golden
Extractor
Field
Solver
Golden
Data
Model
Builder
Processor
Extractor Models
Extractor
e.g. Rapheal, Quickcap, Fast(er)cap
e.g. StarRC, Quantus
OR
Extensive test pattern coverage helps determine which effects are significant
The model builder decides which effects need to be modeled in the extractor
Note: OpenRCX does NOT include explicit Metal Fill in the modeling patterns
Thanks: Dimitris Fotakis and David Overhauser

## Slide 27: Verifying Models
Test
Patterns
(drawn)
Golden
Extractor
Golden
Data
Processor
Extractor Models
Extractor
Extract
Data
Compare
Design
Examples
Golden
Extractor
Golden
Data
Processor
Extractor Models
Extractor
Extract
Data
Compare
Verify using test patterns (once per process)
Verify using sample designs
Thanks: Dimitris Fotakis and David Overhauser

## Slide 28: Extraction Accuracy Plots
Field solver error is generally versus a golden reference field solver (e.g. Quickcap vs. Raphael)
Layout Parameter Extractor (LPE) results are compared versus a field solver and LPE models are generally skewed positive so that net capacitance is never underestimated
Thanks: Dimitris Fotakis and David Overhauser

## Slide 29: OpenRCX Calibration Patterns
Structures to calibrate OpenRCX are relatively simple
  Designed for ~65nm node, in ~2004 !
Coupling capacitances are computed only for same-layer neighbors and parallel diagonal wires
Layers above or below are not necessarily adjacent layers (!)
Min width-centric extraction rules are based on LEF
  Non-min width only used on power nets, not signal nets
  Non-min width infrastructure added in November 2024
Resistance was also based on LEF, not calculated
  Resistance as function of width and spacing added in November 2024
Thanks: Dimitris Fotakis and David Overhauser

## Slide 30: OpenRCX Pattern A
Measure
CC_MC_ML
CC_MC_MR
CC_MC_gnd
R_MC
Coupling Cap = f(M_w, M_s, M)
Grounded Cap = f(M_w, M_s, M)
R_MC
M_w
M_s
ML
MC
MR
M_s
M_w
M_w
Thanks: Dimitris Fotakis and David Overhauser

## Slide 31: OpenRCX Pattern B
Measure
CC_MC_ML
CC_MC_MR
CC_MC_Munder
CC_MC_gnd
Coupling Cap = f(M_w, M_s, M, Munder)
Grounded Cap = f(M_w, M_s, M, Munder)
MC
MR
…
…
M_w
ML
M_w
M_w
M_s
M_s
Thanks: Dimitris Fotakis and David Overhauser

## Slide 32: OpenRCX Pattern C
Measure
CC_MC_ML
CC_MC_MR
CC_MC_Mover
CC_MC_gnd
Coupling Cap = f(M_w, M_s, M, Mover)
Grounded Cap = f(M_w, M_s, M, Mover)
ML
MC
MR
M_s
M_s
M_w
M_w
M_w
Thanks: Dimitris Fotakis and David Overhauser

## Slide 33: OpenRCX Pattern D
Measure
CC_MC_ML
CC_MC_MR
CC_MC_Mover
CC_MC_Munder
CC_MC_gnd
Coupling Cap = f(M_w, M_s, M, Mover, Munder)
Grounded Cap = f(M_w, M_s, M, Mover, Munder)
ML
MC
MR
M_s
M_s
M_w
M_w
M_w
Thanks: Dimitris Fotakis and David Overhauser

## Slide 34: OpenRCX Pattern E
Measure
CC_MC_OC
CC_MC_gnd
Diagonal Cap = f(M_w, M_s, ds, M, Mover)
M_w
M_w
MC
MR
OC
MO_s
OR
ds
MO_w
M_s
Thanks: Dimitris Fotakis and David Overhauser

## Slide 35: Potential Roadmap …
(Deeper dive in May 29 guest lecture: Dimitris Fotakis)
Multi-width and variable spacing
  OpenRCX is written to support this
  Extraction rules need to be expanded
Coupling capacitance to secondary neighbors
  OpenRCX and rules still need to support
Resistance dependent on neighbor
  Merged in November 2024
Lithography effects
  Handled at model creation (drawn to physical) for field solver
Thanks: Dimitris Fotakis and David Overhauser

## Slide 36: Non-Symmetric Coupling to 1st, 2nd Neighbors
w2
w1
w3
s1
s2
Coupling Cap= function(w, s, M), height is set
Fringe (Ground) Cap= function(w, s, M)
M
M
M
CC
Cg
s3
Not currently implemented, but infrastructure exists as of November 2024 (see extFlow_v2, extmain_v2 etc.)
Thanks: Dimitris Fotakis and David Overhauser

## Slide 37: More? E.g., HVH Routing
Measure
CC_MC_ML1
CC_MC_MR1
CC_MC_A1C
CC_MC_A2C
CC_MC_B1C
CC_MC_B2C
CC_A1C_B1C
CC_MC_A2r1
R_MC
Typical density area (50um)2
MC_w
ML_w
MR_w
MR_s
ML_s
ML1
MC
MR1
B2C
A1_w
A1_s
A1C
A2_w
B1_s
B1_w
B1C
A2C
A2_s
B2_w
Ml_n
Mr_n
A2ln
A2rn
A2r1
A2l1
A1f1
A1r1
A1fn
A1rn
B1r1
B1rn
B1f1
B1fn
B2l1
B2ln
B2r1
B2rn
B2_s
…
…
…
…
…
…
…
…
…
…
A2_offset
Thanks: Dimitris Fotakis and David Overhauser